| Product # HER Rectifier Diodes |  | ## Type # HGPW05006-4-01 |  |
| --- | --- | --- | --- |
| ### Metalization # Top Gold  # Bottom Gold  |  |  |  |
| ### Dimension in mils # Dimension. A; 50.5±1mil (1.28+/-0.25mm). B; 33.8±2mil (0.86+/-0.5mm). D; 12±0.6mil (0.3+/-0.02mm). E; 1.5.±1 (.04+/-0.25mm). |  |  |
| Absolute Maximum Ratings (Ta=25℃) ### PEAK REVERSE VOLTAGE VRM .. 400 V FORWARD SURGE CURRENT IFSM….30 A STORAGE TEMPERATURE RANGE Tstg .. –65~150℃ #### Electrical Characteristics Item; Symbol; Test Condition; Standard. FORWARD VOLTAGE(for axial type); VF; IF=1A; 1.25 V (MAX). REVERSE CURRENT; IR; VR=600V; 3μA (MAX). REVERSE RECOVERY TIME; TRR; RG1; 50ns. BREAKDOWN VOLTAGE; BVR; IR=5μA; 440V (MIN). #### Quality Yield Assurance per wafer: 90% |
| YENYO CO.,LTD | Spec No. HGPW05006-4-01 |  | DATE：DEC.03.2001 |