| Product # Super Fast Rectifier Diodes |  | ## Type # SGPW04106-4-01 |  |
| --- | --- | --- | --- |
| ### Metallization # Top Gold  # Bottom Gold  |  | C |  |
| ### Dimension in millimeters # Dimension. A; 1.04-0+0.03mm. B; >0.60mm. C; >0.70mm. D; <0.34mm. E; >0.02mm. F; <0.05mm. |  |  |
| Absolute Maximum Ratings (Ta=25℃) ### PEAK REVERSE VOLTAGE VRM .. 600 V JUNCTION TEMPERATURE Tj ..125℃ PEAK FORWARD SURGE CURRENT IFSM ….20 A STORAGE TEMPERATURE RANGE Tstg .. -65~150℃ #### Electrical Characteristics (sampling 100pcs per 1 lot) Item; Symbol; Test Condition; Standard. FORWARD VOLTAGE; VF; IF=1A; 2.0 V (MAX). REVERSE CURRENT; IR; VR=600V; 2μA (MAX). BREAKDOWN VOLTAGE; BVR; IR=5μA; 600V. REVERSE RECOVERY TIME; TRR; RG1; 25nsec. Chip Yield Assurance : 98% |
| YENYO TECH. CO., LTD. | Spec No. SGPW04106-4-01 |  | DATE: FEB .02.2005 |